## Slide 1: WHAT IS GREASE
“A solid to semifluid product of dispersion of a thickening agent in liquid lubricant. Other ingredients imparting special properties may be included“
It possess a high initial viscosity, which upon the application of shear, drops to give the effect of an oil-lubricated bearing of approximately the same viscosity as the base oil used in the grease.
It is simply a Lubricating fluid which has been gelled with a thickening agent.
+ + =
70-95% Base oil
3-30 % Thickener
10 % Additives
Lubricating Grease

## Slide 2: FUNCTION OF GREASE
Heat dissipation
Corrosion protection
Contaminant removal
Provide a seal preventing environment ingress
It delivers oil via a thickness matrix ( oil reservoir) & keep oil in place.
Fluid level does not have to be controlled and monitored.

## Slide 3: TECHNICAL TERMINOLOGY USED FOR GREASE
Base Oil: The Lubricant dispersed in Thickener, Most greases use mineral based greases or synthetic base oil grease.
Thickener: a material that, in combination with the selected lubricant, will produce the solid to semifluid structure. Various Thickeners are:
  metallic soap : Lithium, Aluminum, Clay, Polyurea, Sodium & Calcium.
  Complex greases : Combination of Metallic Soap with organic complex.
  Non-Soap Thickeners: Bentonite and silica aerogel

## Slide 4: TECHNICAL TERMINOLOGY USED FOR GREASE
Additives: enhance the existing desirable properties, suppress the existing undesirable properties, and impart new properties. The most common additives are:
    oxidation and rust inhibitors
    extreme pressure
    Antiwear
    friction-reducing agents.
Pumpability: ability of a grease to be pumped or pushed through a system. It’s the ease with which a pressurized grease can flow through lines

## Slide 5: TECHNICAL TERMINOLOGY USED FOR GREASE
Water resistance: ability to withstand the effects of water with no change in its ability to lubricate.
Consistency: resistance to deformation by an applied force. The measure of consistency is called penetration. The penetration well depicted by the NLGI ( National Lubrication Grease Institute) in the range of 000 to 6.
Dropping point: the temperature at which a grease becomes fluid enough to drip it indicates the upper temperature limit at which a grease retains its structure.
Oxidation stability: ability to resist a chemical union with oxygen, which will lead to the formation of insoluble gums & sludges.

## Slide 6: WORKING PRINCIPLE
Greases are a type of shear-thinning or pseudo-plastic fluid which means that the viscosity of the fluid is reduced under shear.
After sufficient force to shear the grease has been applied, the viscosity drops and approaches that of the base lubricant and the reduction of shear force with time makes it thixotropic
Thixotropy is shear thinning property. Certain gels or fluids that are thick under static conditions will flow over time when shaken, agitated, or otherwise stressed

## Slide 7: NLGI GRADING OF GREASE
NLGI stands for NATIONAL LUBRICATING GREASE INSTITUTE.
NLGI Classification define 09 (Nine Grades), each determined by the Cone Penetration Test of Lubricating Grease.
The apparatus consists of a closed container and a piston-like Perforated plunger to allow grease to flow.
The test grease is inserted into the container and the plunger is stroked 60 times.
The Container & grease are maintained at a temperature of 25 °C.

## Slide 8: NLGI CONSISTENCY NUMBERS
NLGI No | ASTM ( 60 Strokes Penetration at 25 Deg C, (1/10 of mm) | Appearance
000 | 445-475 | Fluid
00 | 400-430 | Semi Fluid
0 | 355-385 | Very Soft
1 | 310-340 | Soft
2 | 265-295 | Normal grease
3 | 220-250 | firm
4 | 175-205 | Very firm
5 | 130-160 | hard
6 | 85-115 | Very hard

## Slide 9: GREASE SELECTION
1) Determine proper Base oil Viscosity:
use speed factors such as NDm
(NDm = rpm x [(bearing bore + outside diameter) ÷ 2]),
DN [DN = (rpm) x (bearing bore)]
and the operating temperature to derive the minimum vis.cosity requirement
2) Determine the proper grease thickener type and consistency
general-purpose greases will use lithium or lithium-complex thickener
high-temperature applications, bentone or clay thickener is preferred
For heavy water environments, aluminum complex thickener is preferred
3) Determine the proper base oil type

## Slide 10: GREASE SELECTION
4) Determine the proper additive package
anti-wear (AW)
extreme pressure (EP)
rust and oxidation inhibitors (RO)
e.g.
a slow-moving, standard-temperature conveyor bearing may use either an EP or AW
high-speed, high-temperature electric motor will require only AW

## Slide 11: APPLICATION OF GREASE
Greases are applied to mechanisms that can only be lubricated infrequently and where a lubricating oil would not stay in position
They also act as sealants to prevent ingress of water and incompressible materials.
Machinery that runs intermittently or is in storage for an extended period of time.
Machinery that is not easily accessible
Worn components. Grease maintains thicker films

## Slide 12: MAKING OF GREASE
Synthesize the thickener in fluid.
Defined time, Temperature and Mixing pattern is followed
Thorough mixing & blending of Additives at proper time & temperature.
Homogenize the composition.
Passing of grease through a mill to disperse the thickener and additives
De aration of grease to remove the contained air that got mixed during making of grease.

## Slide 13: TYPE OF GREASE USED IN SMP
GREASE SERVO GEM EP2 MAKE SERVO | Coal Crusher_CHP
 | Belt conveyor pulleys Bearings
 | Chines Mill Blower/crusher/clsifier/screw convyor/belt conveyor/Elevator/Belt coupling/Dome Valve Bush/RAV
 | LDO Trnsfer pump Make: Tushco
 | ACW pump make: Kirloskar
 | Fire hydrant pump Maker: kirloskar
 | Boiler fan coupling/bed ash and fly ash silo
GREASE AP3, MAKE-CASTROL | Loop seal blower make: Key international
 | CEP pump
Grease Mobil XHP 222 | Mill Roller Bearings(1mill having 6roller 12brgsmill shaft brg-2points)
SERVO GEM XHT | Boiler Lime Blower
Grease Types
Application in SMP

## Slide 14: GREASE SERVO GEM EP2
EP Stands for “Extreme Pressure” while “2” is the NLGI no.
Servogem EP grease is premium quality Lithium Soap base Product.
Contains Extreme Pressure additives.
It meet the demand of EP grease for boundary lubrication condition so as to prevent excessive wear.
Bears excellent shear stability at low & High load carrying capacity, high oxidation stability & prevent rust & corrosion.
Recommended for the lubrication of both Plain & Antifriction bearings in a wide variety of application.

## Slide 15: TECHNICAL SPECS of GREASE SERVO GEM EP2
Property | Servo gem EP2
Appearance | Smooth Light Brown
Thickener type | Lithium Soap
Base Oil type | Mineral
NLGI class | 2
Worked Penetration at 25 Deg C | 265-295
Drop Point | 180 deg C

## Slide 16: GREASE AP3, MAKE-CASTROL
It is NLGI 3 Lithium Soap Grease containing oxidation and Corrosion inhibitors. The relative low base oil viscosity of AP 3 Makes it an ideal Grease for Lubricating high speed bearings.
Recommended for roller bearings in electric motors & fans.
It has firm Consistency & antio-corrosion performance.
Benefits:
  Light Base Oil Viscousity: ideal for penetrating roller contacts at high speed
  Advanced Corrosion Inhibiting Additives: Protect against Corrosion
  Firm Consistency: Resist water washout & Grease loss due to vibration.

## Slide 17: TECHNICAL SPECS of GREASE AP3
Property | Castrol AP3 Grease
Appearance | Smooth Light Brown
Thickener type | Lithium Soap
Base Oil type | Mineral
NLGI class | 3
Worked Penetration | 225-245 dmm
Drop Point | 180 deg C
Base Oil Viscousity | 70 cSt

## Slide 18: MOBILGREASE XHP 222
XHP Stands for “Extra High Performance ” & 222 is the Base oil Viscosity at 40 Deg Celcius.
This Lithium complex grease provide excellent high temperature performance with superb adhesion, structural stability and resistance to water contamination
have a high level of chemical stability and offer excellent protection against rust and corrosion and excellent oxidation stability
These greases feature high dropping points & operating temperature of 140º C
Mobilgrease XHP 222 Special is an extreme pressure grease fortified with 0.75% molybdenum disulfide that provides protection from wear

## Slide 19: TECHNICAL SPECS OF MOBILGREASE XHP 222
Property | Mobilgrease XHP 222
Appearance | Dark BLue
Thickener type | Lithium Complex
Base Oil type | Mineral oil
NLGI class | 2
Worked Penetration | 280 dmm
Drop Point | 280 deg C
Base Oil Viscousity | 220 cSt at 40 Deg C

## Slide 20: SERVO GEM XHT
XHT Stands for “Extra High Temperature”
Non-soap based smooth structure
Excellent ability to withstand high temperature and severe shock load conditions
These have excellent resistance to water washout and do not get affected by mild acids and alkalies
Servogem HTXX contains MoS2 and has high load bearing ability
Recommended for the lubrication of machine elements, plain bearings and anti-friction bearings operating at high temperatures (120°C - 250°C)

## Slide 21: TECHNICAL SPECS OF SERVOGEM XHT
Property | Servogem XHT
Appearance | Grayish Brown
Thickener | Non Soap Type
Base Oil type | Mineral oil
NLGI class | 2
Worked Penetration | 265 – 295 at 25 Deg C after 60 Strokes
Dropping Point | 280 deg C
Base Oil Viscosity | 220 cSt at 40 Deg C

## Slide 22: CASE STUDY
NSK Corporation, a manufacturer of Rolling element bearing coducted a compatibility study with 10 greases.
For each case, two greases were first tested separately and then blended at three different ratios.
The worked penetration test was used on the greases after being blended at room temperature.
The result shows every grease is compatible with at least one other grease.
The most incompatible were Aluminum complex, calcium complex, clay and Polyurea-thickened greases.

## Slide 23: CASE STUDY
Barium grease blends looked like grease on the bottom and oil on the top which
shows not all thickeners of the same group are compatible with each other

## Slide 24: CHANGEOVER PROCEDURE
Use up as much of the old grease as possible before bringing in the new grease.
While the bearing is running, slowly pump in the new grease until the excess grease being purged.
Run the bearing for one week relubricate using the normal procedure.
Temporarily increase the regrease volume to remove out any remaining old grease
Initiate testing (power consumption, amperage draw, relubrication frequency, vibration, etc.)
sample the purged grease, test its consistency.

## Slide 25: SUBSTITUTION TABLE FOR DIFFERENT GREASE

## Slide 26: HOW MUCH GREASING IS ENOUGH
Measure the size of the bearing shaft, width and bearing outer diameter, as well as the grease gun output per stroke
Gq = 0.114 DB
Where: Gq = Grease quantity in ounces
D = Bearing outside diameter in inches
B = Total bearing width in inches
shaft diameter for bore diameters up to 6, estimate the number of inches in the shaft.
Multiply that number by itself to get a rough estimate of the number of shots from the grease gun.

## Slide 27: TESTING OF GREASE
Static Tests:
  ASTM D-1742 Test Oil Separation from Lubricating Grease During Storage at room temperature.
  ASTM D-6184 Test Method for Oil Separation from Lubricating Grease at Elevated Temperature
  Dynamic Tests:
    U.S. Steel Pressure Oil Separation Test : measure the oil separating tendency & indicate the stability of a grease under high pressures.
    ASTM D-4425 Oil Separation from Grease by Centrifuge: oil separation tendency at high centrifugal forces.

## Slide 28: ADVANTAGE OF GREASE
Spattering is nearly eliminated
Less frequent Application
Easier to handle
Adhere better to the surfaces
Reduce noise & vibration
Widely available,
Excellent flow properties
Even temperature gradient
Provide fresh lube during operation
Allows wear particulate to settle,
Ability to wash contaminants away
Carry away unwanted heat (thermal convection